Re: Supplier verification of compliance to material requirements of AAMA/WDMA/CSA 101/I.S.2/A440-17.

Supplier Name:

Material: Fasteners

Supplier Address:

This document indicates that materials supplied to 		comply with the material requirements in Clause 6 of AAMA/WDMA/CSA 101/I.S.2/A440-17 applicable to all windows, doors, TDDs, and skylights including glazing, sash, panel, leaf and frame materials as listed below;

11.3 Fasteners CPM

There is a commentary available for this Clause.

Fasteners shall be compatible with the materials being fastened, including strength and resistance to corrosion in the intended application. Coatings on carbon steel fasteners other than nails, staples or corrugated fasteners, shall comply with the ASTM standards applicable to the coating type and/or process employed, for the class, type, service condition and/or classification code defined by the window, door, or unit skylight manufacturer.

All externally exposed fasteners shall be tested to ASTM B117 salt spray resistance, for a minimum of 96 hours using visual inspection with no corrosion observed.

Fastening devices used on highly acidic woods, such as, but not limited to, redwood, western red cedar, yellow cypress, and some pressure-treated woods, shall be made of galvanized steel, austenitic, martensitic, or coated ferritic stainless steel, or non-ferrous material.

The surfaces of nails, staples, and corrugated fasteners that are exposed after the product is installed shall be corrosion resistant or protected by a corrosion-resistant coating.

A.11.3 Fasteners CPM

This is a commentary on Clause 11.3

Fasteners must be of a compatible material to the mating surfaces or coated to prevent galvanic reaction. Further information on the capability of fasteners is found in AAMA TIR A9, Section 4 and the Industrial Fastener Institute’s Fastener Standards. For coastal and other high exposure applications, specifiers should consider fasteners and hardware that meets higher levels and alternative tests for corrosion resistance.

Acknowledgement of compliance:

Signature:_________________________ 			Date_________________

Position:__________________________

References: North American Fenestration Standard / Specification for windows, doors, and skylights. AAMA/WDMA/CSA 101/I.S.2/A440-17